## Slide 1: Tutorial: Atomic Layer Deposition for Photovoltaics (ALD4PV)
Dr. Bart Macco
Department of Applied Physics

## Slide 2: Four take-away messages up front
  The field of ALD4PV is too big to cover fully in 45 mins.
  ALD is already big in the solar industry.
  Various merits of ALD play a key role in many cell concepts.
  High-quality PV materials can be made by doing “smart ALD”.

## Slide 3
~5 nm ALD Al2O3 layers
1-3 wafers/sec
~0.01-0.03 $ per wafer
Solaytec spatial ALD
Leadmicro batch ALD
Al2O3
Leadmicro: “Almost all major PV cell manufacturers in China now use our system.”
Silicon
metallization
SiNx
Silicon
local p+ Si
Al2O3/SiNx stacks
n+ Si
Al2O3

## Slide 4
ZnO
ZnO
New materials & concepts in research!
Gigawatts of ALD Al2O3 passivation layers in industry!
ALD Transparent
conductive oxides
(TCOs)
ALD4Perovskites
and tandems
Al2O3
Silicon
Al2O3/SiNx stacks
Al2O3

## Slide 5: ALD merits: Thickness control, uniformity, conformality, …
Thickness control
Uniformity
Conformality
Many materials
Examples of where these merits really matter throughout the tutorial!

## Slide 6: ALD merits: A wide variety of materials
For PV, most interesting:
Metal oxides
Metal (oxy)sulfides
Metal nitrides
(Examples to come…)
New interactive online ALD database:
www.Atomiclimits.com

## Slide 7: Outline
  A solar cell crash course
  ALD4SiPV: From passivation layers to passivating contacts
  ALD4TCOs: Transparent conductive oxides
  ALD4Perovskite (tandems)
  Personal outlook

## Slide 8: A solar cell crash course
Semiconductor (Si, …)
Photogeneration of excess electrons and holes in semiconductor
upon light absorption
On opposite sides, regions (often thin films)
that let only electrons or holes pass
Extract current via external circuit
External load
hν
hν
hν
hν
hν
hν

## Slide 9: ALD4SiPV: From passivation layers to passivating contacts

## Slide 10: Basics of surface passivation
Semiconductor (Si, …)
Valence band
Conduction band
hν
Photogeneration of excess electrons and holes
Recombination, mainly through surface defects
Equilibrium concentration by balance of generation and recombination
electrons
holes

## Slide 11: Basics of surface passivation
Use thin films to reduce recombination at surface of semiconductor.
Chemical passivation: Reduce # of surface defects
Valence band
Conduction band
electrons
holes
H
Thermal annealing
Dielectric
e.g. Al2O3
silicon
SiOx
H
Thermal annealing
ALD Al2O3
Surface defect states

## Slide 12: Basics of surface passivation
Use thin films to reduce recombination at surface of semiconductor.
Chemical passivation: Reduce # of surface defects
Field-effect passivation: Repel one type of charge carrier
Valence band
Conduction band
electrons
holes
Dielectric
e.g. Al2O3
silicon
ALD Al2O3
SiOx
Negative interfacial
trapped charge
E-field
Negative interfacial
trapped charge
Easiest to repel the minority carrier:
n-type silicon  positive fixed charge
p-type silicon  negative fixed charge

## Slide 13: From Al-BSF to PERC
Used to be the industrial standard
Limited by recombination at the rear metal-silicon interface
Al-BSF cell, efficiency ~20%
PERC cell, efficiency ~22-23%
New industrial standard
Rear side mostly passivated by Al2O3/SiNx, with small local metal-silicon contacts
metallization
SiNx
c-Si wafer (textured)
local p+ Si
p+ Si
Al2O3/SiNx stacks
n+ Si

## Slide 14: Trends in silicon photovoltaics
Black silicon
New passivation materials
Passivating contacts
Many more …
metallization
SiNx
c-Si wafer (textured)
local p+ Si
n+ Si
Al2O3/SiNx stacks
c-Si
SiOx
TiOx
c-Si
SiOx
Poly-Si
ALD Al2O3

## Slide 15: ALD for passivation of black silicon
Black silicon: Nanotextured surface
H. Savin et al., Nat. Nanotechnol., 10, 7, 624–628, 2015.
van de Loo et al., Appl. Phys. Lett. 110, 263106 (2017)
Ref book chapter
Conformality of ALD Al2O3 crucial for coating pillars
Although not very common, you can buy such modules
e.g. Trina ALLMAX-PD05.05
Standard pyramid texture

## Slide 16: A brief history of silicon passivation layers
[1] Jäger and Hezel, Proc. 18th IEEE PVSC, Las Vegas, pp. 1752–1753, 1985.
[2] B. Hoex et al., Appl. Phys. Lett., vol. 89, no. 4, p. 042112, 2006.
[3] G. Agostinelli et al., Sol. Energy Mater. Sol. Cells, vol. 90, no. 18–19, pp. 3438–3443, Nov. 2006.
[4] Feldmann et al, ”Sol. Energy Mater. Sol. Cells, vol. 131, pp. 46–50, 2014.
[5] Black et al., Sol. Energy Mater. Sol. Cells, vol. 188, no. June, pp. 182–189, 2018.

## Slide 17: Many new ALD materials for passivation: POx/Al2O3
Defect density
Fixed charge
Good for n-type Si
Good for p-type Si
Unique:
Strong positively
charged oxide!
Adapted from Cuevas et al.
Nb2O5

## Slide 18: Many new ALD materials for passivation: POx/Al2O3
Precursors: Trimethylphosphate (TMP) & TMA + O2 plasma
Black et al,. Appl. Phys. Lett. 2018, 112 (20), 201603.
Black et al., Sol. Energy Mater. Sol. Cells 2018, 185 (March), 385–391.
As good as best SiNx on n-type surfaces
Thanks to positive fixed charge
c-Si(p)
n+ FSF
p+ LBSF
POx/AlOx
SiNx
Front side PERC cell? & laser P dopant source?

## Slide 19: Many new ALD materials for passivation: conductive ZnO
State-of-the-art passivation (~730 mV)
Unique: a very conductive passivation layer!  Opens up new cell concepts
Soft ALD deposition is key
Tunnel oxide for chemical passivation cannot withstand plasma PVD, …
Perfect doping control by ALD
Doping helps field-effect passivation
Doping helps tunneling over oxide
van de Loo et al., J. Appl. Phys., vol. 125, no. 10, p. 105305, 2019

## Slide 20: From passivation layers to passivating contacts
semiconductor
Valence band
Conduction band
External load
e-h
recombine
e-selective
membrane
h-selective
membrane
A passivating contact:
A layer that passivates the silicon surface, selectively letting one carrier type (e/h) pass
Can be achieved in various ways:
Doping, band offsets, work function difference, …
Beyond the scope to explain mechanisms,
see “Further reading” slides

## Slide 21: Passivating contacts based on ALD metal oxides
metallization
SiNx
c-Si wafer (textured)
p+ Si
TiO2 as e-selective contact
 22.1% efficiency
Yang et al., Progress in Photovoltaics: Research and Applications, 25(11), 896–904 (2017)
Simple and cheap ALD!
TiCl4, H2O, 75 oC
n-type Si
EF
metal
TiO2
Only 3 nm needed
ALD: Thickness control,
6” uniformity
Works by conduction band alignment
c-Si
SiOx
TiOx

## Slide 22: Poly-Si passivating contacts
metallization
Al2O3/SiNx
c-Si wafer (textured)
1F. Feldmann, https://www.atomiclimits.com/2018/07/23/looking-back-at-the-passivating-contact-workshop-in-eindhoven-passivating-contact-materials-based-on-silicon/
2https://www.pv-tech.org/products/trina-solar-launches-425wp-bifacial-i-topcon-module
2019:
Buy them!2
cell > 24%
2013: Rediscovered by F-ISE1
Concept borrowed from transistors
in the 80s! (SIPOS)
p+ Si
c-Si
SiOx
Poly-Si(n)

## Slide 23: Hydrogenation layers for poly-Si contacts
M. Schnabel et al., Appl. Phys. Lett., 112, 20, 203901 2018.
B.W.H. van de Loo et al., (submitted)
Voltage
666 mV
688 mV
712 mV
As-dep
Forming
gas anneal
ALD Al2O3
+anneal
Hydrogenation of tunnel oxide is crucial for chemical passivation!
ALD Al2O3 has proven to be an excellent hydrogenation source!
c-Si
SiOx
Poly-Si
ALD Al2O3
H H H H

## Slide 24: To sum up this part…
Black silicon
Novel passivation materials
c-Si
SiOx
TiOx
Passivating contacts
ALD is already
big in industry ….
And very much present in novel concepts!
ALD Al2O3 in PERC
TODO: Change to PERC cell and add timeline fig Aaf
c-Si wafer (textured)

## Slide 25: ALD4TCOs: ALD for transparent conductive oxides

## Slide 26: Basics of transparent conductive oxides (TCOs)
TCOs found in many cell types for lateral electrical transport.
Mostly sputtering (PVD)
Transparency: Wide bandgap host (~>3 eV)  In2O3, ZnO, SnO2, …
Conductivity: Dopants  Sn, Al, B, F, H, …  ρ ~< 1 mΩcm
CIGS
Perovskite
Si heterojunction
EF
Intrinsic
host
EF
+ doping
VB
CB
BM-shift
Free carrier absorption

## Slide 27: 3 challenges and opportunities for ALD TCOs
e-
Avoid substrate damage
by “soft deposition”
Make high mobility TCOs by avoiding scattering
Achieve efficient doping by avoiding dopant clustering

## Slide 28: Making doped TCOs by ALD: The supercycle approach
time
DEZ
H2O
purge
DMAI
H2O
purge
ZnO
Al doping
n cycles
1 cycle
precursor
reactant
1 supercycle
purge
n cycles host TCO
1 cycle dopant
Digital doping control
Ne = 7∙1019-1∙1021 cm-3
Wu et al. (2013). Chemistry of Materials, 25(22), 4619–4622.
DMAI
ZnO:Al from DEZ and DMAI

## Slide 29: The case of ALD Al-doped ZnO
Clustered dopants
Low doping efficiency
Dispersed dopants
Enhanced doping efficiency
Vertical control by supercycle ratio
TMA doping in ZnO
How to achieve more lateral spacing?
Or: How to reduce #Al atoms/cycle?

## Slide 30: The case of ALD Al-doped ZnO
Achieve less Al/cycle by cycle modifications:
Partially block TMA absorption by dosing alcohols prior to TMA1
Omit H2O dose before TMA2
3. Introduce a long wait step before TMA => dehydroxylation13
ZnO
OH
OH
OH
OH
OH
EtOH
OH
EtOH
OH
OH
EtOH
Al(CH)x
EtOH
EtOH
Al(CH)x
Al(CH)x
TMA
OH
ZnEt
OH
OH
ZnEt
TMA
Al(CH)x
ZnEt
ZnEt
Al(CH)x
Al(CH)x
ZnO
OH
OH
OH
OH
OH
Al(CH)x
Al(CH)x
Al(CH)x
TMA
OH
H2O
O
OH
WAIT
H2O
O
O
O
Yanguas-Gil et al., Chem. Mater. 2011, 23, 4295–4297.
Na et al. Chem. Mater. 2009, 21 (6), 5585–5593.
Park et al., Appl. Surf. Sci. 2014, 309, 133–137.

## Slide 31: The case of ALD Al-doped ZnO
4. Use steric hindrance of bulkier dopant precursors
Clustered dopants
Low doping efficiency
Dispersed dopants
Enhanced doping efficiency
Low steric hindrance
High # Al atoms nm-2 cycle-1
OH
OH
OH
OH
OH
O
OH
Al
CH3
CH3
Enhanced steric hindrance
Low # Al atoms nm-2 cycle-1
OH
OH
OH
OH
OH
O
OH
Al
HC
CH3
CH3
CH3
O
TMA
as dopant precursor
“Bulkier” DMAI
as dopant precursor
~11 Al atoms/nm2·cycle
Doping efficiency = 5-10%
Resistivity = 2.4 mΩ·cm
~0.3 Al atoms/nm2·cycle
Doping efficiency = >30%
Resistivity = 0.7 mΩ·cm
Wu et al., Chem. Mater. 2013, 25 (22), 4619–4622.
Macco et al., Semicond. Sci. Technol. 2014, 29 (12), 122001.

## Slide 32: DMAI: Al-doped ZnO in silicon heterojunction cells
Niemelä et al., Sol. Energy Mater. Sol. Cells 2019, 200, 109953.
ITO
a-Si:H (i/n)
a-Si:H (i/p)
c-Si(n)
Replace scarce indium-tin-oxide (ITO)
with abundant ALD ZnO:Al at the rear
ITO  ZnO:Al
Both ITO and ZnO:Al
efficiency of 21.3%

## Slide 33: High-mobility ALD TCOs
Scattering at grain boundaries limits the mobility.
Mitigate grain boundary scattering by:
Enhancing grain size
Passivating boundaries with hydrogen
H
H
H
H
H
e-
A high mobility μ allows for a low carrier density Ne
A high carrier density  free carrier absorption
e-
35 cm2/Vs
138 cm2/Vs

## Slide 34: High-mobility ALD TCOs: ZnO:H
Use supercycles of ZnO with H2 plasma
time
DEZ
H2O
purge
H2 plasma
ZnO cycle
Doping/etching
n cycles
1 cycle
precursor
reactant
1 supercycle
purge
Substrate
Etching H2 plasma
The H2 plasma:
Dopes the ZnO with H
Reduces grain competition by etching nuclei:
~3 at. %
Macco et al, SOLMAT 173 (2017) 111-119
Macco et al., Semicond. Sci. Technol. 29 (2014) 122001
Demaurex et al., IEEE J. Photovoltaics. 4 (2014) 1387–1396.

## Slide 35: High-mobility ALD TCOs: ZnO:H
Without H2 plasma
TEM cross-section
With H2 plasma
With H2 plasma
No H2 plasma
H2 plasma : Tune delay!
Mobility 27 cm2/Vs
Mobility 48 cm2/Vs
(Max mobility ~ 55 cm2/Vs

## Slide 36: High-mobility ALD TCOs: In2O3:H
Anneal 150-200 oC
High-mobility and polycrystalline In2O3:H
μ=130 cm2/Vs
100 oC
200 oC
Amorphous + embedded crystallites
μ=37 cm2/Vs
“semicrystalline”
μ=68 cm2/Vs
polycrystalline
μ=35 cm2/Vs
Tdep
Precursor
H2O + O2
InCp
Reactants
HIT-cell2 +1.7 mA/cm2
1 Macco et al, Journal of Applied Physics 120(8) 085314 (2016)
2 Y. Kuang et al., Sol. Energy Mater. Sol. Cells, 163, January, 43–50, 2017.
3 Keller et al., Prog. Photovoltaics Res. Appl., 24, 1,102–107, 2016.
CIGS:3
+1.7 mA/cm2

## Slide 37: Soft deposition of ALD TCOs
Sputtering: Energetic ions and photons can create defects in passivation layer.
Thermal ALD  No plasma defects!
Silicon heterojunction
Cell mask layout
Sputter TCO:
Sputter damage
ALD TCO:
No damage

## Slide 38: Soft deposition of ALD TCOs
Soft deposition is growing increasingly important for newer cell concepts
ZnO:B
c-Si
SiO2
a-Si:H passivation:
~Full recovery
by annealing1
Poly-Si passivation:
Partial recovery
by annealing2
Perovskites
killed
by plasma3
Tunnel SiO2/ZnO
SiO2 killed
by plasma4
1 Demaurex et al., Appl. Phys. Lett., vol. 101, no. 17, p. 171604, 2012.
2 Tutsch et al., Sol. Energy Mater. Sol. Cells, vol. 200, no. May, p. 109960, 2019.
3 Zardetto et al., Sustain. Energy Fuels, vol. 1, no. 1, pp. 30–55, 2017.
4 van de Loo et al., J. Appl. Phys., vol. 125, no. 10, p. 105305, 2019

## Slide 39: ALD for perovskite and tandems

## Slide 40: The rise of perovskite and Si-perovskite tandems
Impressive efficiency rise
for perovskite & Si-perovskite tandems
Perovskite
Silicon

## Slide 41: ALD SnO2 as buffer layer in c-Si/perovskite tandems
~10-20 nm ALD SnO2 used in recent record tandems 1,2,3
[1] E. Köhnen et al., Sustain. Energy Fuels, 2019.
[2] M. Jošt et al., Energy Environ. Sci., 2019.
[3] F. Sahli et al.,” Nat. Mater., Jun. 2018.
+ Soft sputter protection layer
+ Conformal, low-pinhole density layer for environmental stability

## Slide 42: ALD on challenging perovskite “substrates”
1 Tan et al., ACS Appl. Mater. Interfaces, 10, 6, 5485–5491, 2018.
2 Zardetto et al., Sustain. Energy Fuels, 1, 1, 30–55, 2017.
3 Hultqvist et al., ACS Appl. Mater. Interfaces, 9, 35, 29707–29716, 2017.
4 Palmstrom et al., Adv. Energy Mater., p. 1800591, 2018.
Thermal stability1
Limit thermal budget!
Or “quick” processing
No plasma processes2
Chemical stability3,4
Precursors can react with perovskite
DEZ
TMA
TDMASn

## Slide 43: ALD for interface engineering of perovskites
Ultrathin ALD Al2O3 on perovskite
Koushik et al., Energy & Envir.Science, 10, 91-100 (2017)
Koushik et al, Advanced Mat. Interfaces 1700043 (2017)
Perovskite
Al2O3
Spiro-OMeTAD
+ “Passivation”
- Too thick for tunneling
Conformal
Passivating
while allowing for tunneling
Stabilizing
Moisture barrier
Dry N2
40% RH
60% RH
50-70% RH

## Slide 44: Conformal ALD NiO for CIGS/Perovskite tandem
M. Jost et al.,” ACS Energy Lett., p. acsenergylett.9b00135, 2019.
18.2%
21.6%
PTAA
only
ALD NiO
only
ALD NiO
+ PTAA
3.6%
Roughness up to 1 µm
 Pinholes for solution-processed PTAA hole-contact
Solution: Introduce conformal, pinhole-free ALD NiO hole-contact
Efficiency:

## Slide 45: Summary & Personal outlook
ALD has made it’s mark in photovoltaics!
Personal view:
“The further we creep toward the efficiency limits, the more the atomic-level of control that ALD offers starts to matter.“
ALD Al2O3 in industry
Novel passivation layers and passivating contacts
High quality TCOs & soft deposition
ALD4Perovskite

## Slide 46: Thank you for your attention!
Special thanks to:
The PMP-group
Erwin Kessels
Adriana Creatore
Jimmy Melskens
Bas van de Loo
Dibya Koushik
And many others for contributing!

## Slide 47: Extra slides

## Slide 48: Further reading
Physics of solar cells and passivating contacts:
P. Würfel, Physics of Solar Cells. Wiley, 2005.
U. Wurfel, et al., “Charge Carrier Separation in Solar Cells,” IEEE J. Photovoltaics, vol. 5, no. 1, pp. 461–469, 2015.
J. Melskens et al., “Passivating Contacts for Crystalline Silicon Solar Cells: From Concepts and Materials to Prospects,” IEEE J. Photovoltaics, vol. 8, no. 2, pp. 373–388, Mar. 2018.

## Slide 49: Further reading
Silicon passivation
L. E. Black et al., “Explorative studies of novel silicon surface passivation materials : Considerations and lessons learned,” Sol. Energy Mater. Sol. Cells, vol. 188, no. June, pp. 182–189, 2018.
G. Dingemans et al., “Status and prospects of Al2O3-based surface passivation schemes for silicon solar cells,” J. Vac. Sci. Technol. A Vacuum, Surfaces, Film., vol. 30, no. 4, p. 040802, 2012.
TCOs:
M. Morales-masis et al., “Transparent Electrodes for Efficient Optoelectronics,” 2017.

## Slide 50: Field-effect passivation
Field-effect passivation: Charge in the layer attracts/repels minority carriers
Bottom line, use negative Qf (Al2O3) for p-type, positive Qf (SiNx) for n-type Si
Macco et al., ALD in Energy Conversion Applications, Wiley, 2017